## Slide 1
Development of Retro-Reflective Materials for Building Coatings
Research Introduction
Reporter: Jihui Yuan
Date：2025.07.21

## Slide 2
Introduction
RRM vs Traditional Materials
01
02
RRM Development
03
Durability Testing
04
Urban Canyon Albedo Simulation
05
Thermal Load Simulation
06
目录
CONTENTS
Conclusions
07
Future Work
08

## Slide 3
Introduction
01

## Slide 4
Urban Heat Island Mitigation
Buildings contribute to ~50% of urban heat emissions, exacerbating urban heat islands. High solar reflectivity materials are essential for reducing cooling energy demand and improving air quality.
Heat Emissions from Buildings
Retro-reflective materials (RRM) reflect light back to its source, unlike traditional diffuse reflective materials. This unique property can significantly reduce heat transfer to neighboring areas.
RRM Concept

## Slide 5
RRM vs Traditional Materials
02

## Slide 6
Diffuse reflection scatters light in multiple directions, leading to higher heat absorption by surrounding surfaces. This is less effective in reducing urban heat islands.
Diffuse Reflection
RRM reflects light back to its source, minimizing heat transfer to adjacent buildings and roads. This enhances urban canyon albedo more effectively.
Retro-Reflection
Reflection Mechanisms

## Slide 7
RRM Development
03

## Slide 8
The new RRM features a glass covering with high transmittance and strength, ensuring durability and high reflective luminance.
Glass Covering
Plastic micro-prisms with cubic corners replace traditional glass beads, providing a white appearance and strong UV resistance.
Plastic Micro-Prisms
Material Composition

## Slide 9
Durability Testing
04

## Slide 10
After 485 days of outdoor exposure, the solar reflectance (ρtmp) remained at ~0.81, demonstrating excellent durability.
Solar Reflectance
The retro-reflectance (ρret) remained at ~0.44, with no surface degradation observed under a microscope.
Retro-Reflectance
Outdoor Testing Results

## Slide 11
Urban Canyon Albedo Simulation
05

## Slide 12
Simulation Results
A 2D model showed that RRM on both walls (Case C) achieved the highest urban canyon albedo, outperforming diffuse and mirror materials.
Albedo Comparison
RRM effectively increases urban canyon albedo, reducing the urban heat island effect by reflecting more sunlight back to the source.
Impact on Urban Heat Islands

## Slide 13
Thermal Load Simulation
06

## Slide 14
Energy Savings
In Shanghai, buildings with RRM coatings experienced a 19% reduction in annual cooling loads, with cooling loads decreasing by 13-15% in summer.
Cooling Load Reduction
Heating loads increased by 5-7% in winter, but the net annual thermal load reduction was 4.3%, with CO₂ emissions reduced by ~3.3 kg/m²-year.
Heating Load Increase

## Slide 15
Conclusions
07

## Slide 16
Summary of Findings
The developed RRM with a glass covering maintained high reflectance for over 485 days, outperforming other materials in durability tests.
Durability and Performance
RRM effectively reduces cooling loads and urban heat islands, with a net reduction in annual thermal loads and CO₂ emissions, making it a promising solution for urban environments.
Energy and Environmental Benefits

## Slide 17
Future Work
08

## Slide 18
Research Directions
Continue testing RRM durability beyond 485 days to further validate long-term performance.
Extended Durability Testing
Develop additional RRM formulations to optimize performance and explore applications beyond vertical walls.
New Formulations
Conduct field testing in real urban environments to assess practical benefits and challenges.
Real-World Applications

## Slide 19
THANKYOU
Reporter: Jihui Yuan
Date：2025.07.21